Sheet Resistance Specification and Lot Acceptance

SPEC-RS-118  |  Rev D

This specification sets the sheet resistance (Rs) target and limits after the RTA activation anneal, the within-wafer nonuniformity definition, the site bin thresholds, and the lot acceptance criteria. The site measurement pattern and the site exclusion and retest rules are defined in the Sampling Plan (SP-RS-045). This specification does not restate them. Rs values are in ohms per square.

CONFIDENTIAL - INTERNAL PROCESS ENGINEERING.

1   Sheet Resistance Limits

The Rs target is 85 ohm/sq. The specification limits are plus or minus 5 percent of target. A site is within specification when its Rs is greater than or equal to the lower limit and less than or equal to the upper limit; a site outside either limit is a failing site.

| Parameter | Value |
| --- | --- |
| Target Rs | 85.00 ohm/sq |
| Tolerance | +/- 5 % of target |
| Lower spec limit (LSL) | 80.75 ohm/sq |
| Upper spec limit (USL) | 89.25 ohm/sq |

2   Within-Wafer Nonuniformity

Within-wafer nonuniformity (WIW NU) is computed over the included sites of a wafer, after the site exclusion rule in the sampling plan has been applied. The definition used for lot acceptance is the half-range definition:

WIW NU (%) = (Rs_max - Rs_min) / (2 x Rs_mean) x 100

where Rs_max, Rs_min, and Rs_mean are taken over the included sites of that wafer. Do not use a standard deviation-based definition for acceptance. The half-range definition above is the controlling one. A wafer passes the uniformity criterion when its WIW NU is at or below 5.0 percent.

3   Site Bins

Each included site is binned by its Rs relative to target. The warn band flags sites that are within specification but more than 3 percent from target.

| Bin | Condition | Meaning |
| --- | --- | --- |
| PASS | within 82.45 to 87.55 ohm/sq | within 3 % of target |
| WARN | in spec but outside the PASS band (>= 80.75 and <= 89.25) | 3 % to 5 % from target |
| FAIL | below 80.75 or above 89.25 ohm/sq | out of specification |

4   Wafer and Lot Acceptance

Wafer-to-wafer (W2W) variation is computed from the per-wafer mean Rs across the lot, over included sites only. It is reported as a half-range percentage of the lot mean:

W2W (%) = (mean_max - mean_min) / (2 x lot_mean) x 100

Lot yield is the count of included sites within specification across all wafers, divided by the total count of included sites across all wafers.

Wafer uniformity criterion: WIW NU at or below 5.0 percent.

Wafer-to-wafer criterion: W2W at or below 3.0 percent.

Lot yield criterion: at or above 95.0 percent of included sites within specification.

A lot that meets all three criteria is dispositioned CONTINUE. A lot that misses any criterion is placed on HOLD for engineering review.